## PRODUCT DATA SHEET

### CleanTek Defender Coverall With Hood

- Description

  - Coverall with hood

  - Colour: White

  - Zip Closure

  - Elasticated wrists, ankles and back

  - Material: Spunbound Polypropylene

  - Weight: 50 gsm

  - Sewing Thread: 150D polyester filament yarn

- Packaging

1 pce per bag

25 bags per case

- Physical Data

| Property | Unit | Average | Min Value Indiv | Max value Indiv | Method |
| --- | --- | --- | --- | --- | --- |
| Basic Weight | gsm | 49.13 | 47.89 | 50.10 | As Comment |
| MD Tensile Strength | N/5cm | 146.20 | 138.00 | 162.00 | As Comment |
| CD Tensile Strength | N/5cm | 84.20 | 78.00 | 90.00 | As Comment |
| MD Elongation | % | 100.60 | 80.00 | 120.00 | As Comment |
| CD Elongation | % | 99.60 | 78.00 | 113.00 | As Comment |
| Comment: |  |  |  |  |  |  |  |
| 1. Basic Weight Test: [sample size] 100mm×100mm |  |  |  |  |
| 2. Tensile&Elongation Test: [sample size] 200mm×50mm, [test speed] 300 mm/min, [jaw separation] 100 mm |

Note: The physical properties mentioned above represent typical values of nonwoven fabric. These values should not be considered as specification or certificate of material and/or specification values

# Glossary Of Terms

MD: The long direction of the material as it is made on the machine. Called machine direction.

CD: The width of the material as it is made. Called cross machine direction.

Basis Weight: Weight of the material in grammes per square meter.

Tensile Strength: The strength of the textile when it is pulled in one direction. Basically if you hold the material in your hands and pull one end, the amount of “force” you can pull without having the fibres begin to stretch and get narrower.

Elongation: The strength of the textile when it is pulled in one direction and it is the point where the fibres begin to get thinner. Basically if you hold the material in your hands and pull one end, the amount of “force” you can pull to have the fibres begin to stretch and get narrower. This is expressed as a percentage of Tensile Strength.