## PRODUCT DATA SHEET

### CleanTek Sentry Coverall With Hood

- Description

  - Coverall with hood

  - Colour: White

  - Zip Closure

  - Elasticated wrists, ankles and back

  - Material: Polyethylene (PE)

  - Weight:  40 gsm

  - Sewing Thread: 150D polyester filament yarn

- Physical Data

|  | Units | Sample Results | Reference Test Procedure ASTM Standard |
| --- | --- | --- | --- |
| Basis Weight | oz./yd. (gsm) | 1.5 (40) | D3776 |
| Thickness | mils. | 6.77 | D1777 |
| Strip Tensile (MD/CD) | lbs./in. | 8.73/6.22 | D1682 |
| Strip Elongation (MD/CD) | % | 112/107 |  |
| Work to Break (MD/CD) | in. - lbs. | 20.38/12.13 | D1682 |
| Work up to Fmax. (MD/CD) | in. - lbs. | 18.55/10.83 |  |
| Tongue Tear (MD/CD) | lbs. | 15.25/9.62 | D2261 |
| Flammability |  | Class1 | CS-191-53, Sec. 1610 |
| Mullen Burst | lbs./sq. in. | 83 |  |
| Particulate Burden |  | none |  |
| Shrink Temperature | F/Centigrade | 270/132 |  |
| Melt Temperature | F/Centigrade | 275/135 |  |
| Water Vapour Transmission | grams/24 Hours | 360 |  |

Test Date: April 13, 2001

Test Place: PGI NanXin Lab

- Packaging

1 pce per bag

25 bags per case

# Glossary Of Terms

MD: The long direction of the material as it is made on the machine. Called machine direction.

CD: The width of the material as it is made. Called cross machine direction.

Basis Weight: Weight of the material in ounces per square yard.

Thickness of the material: Self-explanatory. In 1000ths of an inch

Strip Tensile: The strength of the textile when it is pulled in one direction. Basically if you hold the material in your hands and pull one end, the amount of “force” you can pull without having the fibres begin to stretch and get narrower.

Strip Elongation: The strength of the textile when it is pulled in one direction and it is the point where the fibres begin to get thinner. Basically if you hold the material in your hands and pull one end, the amount of “force” you can pull to have the fibres begin to stretch and get narrower. This is expressed as a percentage of Strip Tensile.

Work to Break: The amount of force needed to have the material “break” or tear apart when pulling. (Note our values are very high and this is good)

Work up to Fmax: This is the amount of force needed to have the material begin to show signs of breaking.

Tongue Tear: With the material held in place on a flat surface and held down tight, another clamp with material clamped in it pulls vertically. This is the measurement of how much force that it takes to tear the fabric perpendicularly. Like getting the fabric snagged on a bolt and the wearer is walking away. The tongue tear is the amount of force needed to tear the fabric.

Flammability: Class rating for flame.

Mullen Burst: The amount of force required to push a 2” diameter flat rod through the material. This would be like forcing your elbow through the fabric.

Particulate burden: The number of particles less than 3 microns in diameter that can pass through. Three microns is the size of a virus.

Shrink Temperature: The upper limit on heat that can be applied before the material starts to shrink.

Melt Temperature: The upper limit on the amount of heat that can be applied before the fabric melts.

Water Vapour Transmission: The amount of water that can pass through the material over a 24-hour period.